# Text boxes

State at 25°C:	gas

Density: 	0.0001 g/cm3

Melting Point:	14.06 K

Boiling Point: 	20.4 K

Electron Affinity:	72.7711 kJ/mol

1st Ion Energy:	1312 kJ/mol

Electronegativity:	2.20

Atomic Radius:	37.1 pm

1.00794

-1

+1

Hydrogen

1

H

State at 25°C:	gas

Density: 	0.0002 g/cm3

Melting Point:	0.8 K

Boiling Point: 	4.2 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	2372.3 kJ/mol

Electronegativity:

Atomic Radius:	31 pm

4.0026

Helium

2

He

State at 25°C:	solid

Density: 	0.534 g/cm3

Melting Point:	453.74 K

Boiling Point: 	1620 K

Electron Affinity:	59.63 kJ/mol

1st Ion Energy:	520.2 kJ/mol

Electronegativity:	0.98

Atomic Radius:	152 pm

6.941

+1

Lithium

3

Li

State at 25°C:	solid

Density: 	1.848 g/cm3

Melting Point:	1551.2 K

Boiling Point: 	2773 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	899.4 kJ/mol

Electronegativity:	1.57

Atomic Radius:	112 pm

9.01282

+2

Beryllium

4

Be

State at 25°C:	solid

Density: 	2.35 g/cm3

Melting Point:	2352.2 K

Boiling Point: 	3923.2 K

Electron Affinity:	26.7 kJ/mol

1st Ion Energy:	800.6 kJ/mol

Electronegativity:	2.04

Atomic Radius:	85 pm

10.811

+3

Boron

5

B

State at 25°C:	solid

Density: 	2.266 g/cm3

Melting Point:	3823.2 K

Boiling Point: 	5100 K

Electron Affinity:	121.85 kJ/mol

1st Ion Energy:	1086.4 kJ/mol

Electronegativity:	2.55

Atomic Radius:	77.2 pm

12.011

-4

+4

Carbon

6

C

State at 25°C:	gas

Density: 	0.0012 g/cm3

Melting Point:	63.34 K

Boiling Point: 	77.4 K

Electron Affinity:	7 kJ/mol

1st Ion Energy:	1402.3 kJ/mol

Electronegativity:	3.04

Atomic Radius:	70 pm

14.0067

-3

+3

+5

Nitrogen

7

N

State at 25°C:	gas

Density: 	0.0014 g/cm3

Melting Point:	54.8 K

Boiling Point: 	90.2 K

Electron Affinity:	140.9788 kJ/mol

1st Ion Energy:	1313.9 kJ/mol

Electronegativity:	3.44

Atomic Radius:	73 pm

15.9994

-2

Oxygen

8

O

State at 25°C:	gas

Density: 	0.0017 g/cm3

Melting Point:	53.58 K

Boiling Point: 	85.1 K

Electron Affinity:	328 kJ/mol

1st Ion Energy:	1681 kJ/mol

Electronegativity:	3.98

Atomic Radius:	72 pm

18.9984032

-1

Fluorine

9

F

State at 25°C:	gas

Density: 	0.0009 g/cm3

Melting Point:	24.53 K

Boiling Point: 	27.1 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	2080.6 kJ/mol

Electronegativity:

Atomic Radius:	71 pm

20.1797

Neon

10

Ne

State at 25°C:	solid

Density: 	0.968 g/cm3

Melting Point:	371.01 K

Boiling Point: 	1154.6 K

Electron Affinity:	52.868 kJ/mol

1st Ion Energy:	495.8 kJ/mol

Electronegativity:	0.93

Atomic Radius:	186 pm

22.989768

+1

Sodium

11

Na

State at 25°C:	solid

Density: 	1.738 g/cm3

Melting Point:	922 K

Boiling Point: 	1378 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	737.7 kJ/mol

Electronegativity:	1.31

Atomic Radius:	160 pm

24.305

+2

Magnesium

12

Mg

State at 25°C:	solid

Density: 	2.699 g/cm3

Melting Point:	933.57 K

Boiling Point: 	2740 K

Electron Affinity:	42.6 kJ/mol

1st Ion Energy:	577.6 kJ/mol

Electronegativity:	1.61

Atomic Radius:	143 pm

26.98

+3

Aluminum

13

Al

State at 25°C:	solid

Density: 	2.336 g/cm3

Melting Point:	1683.2 K

Boiling Point: 	3553 K

Electron Affinity:	133.6 kJ/mol

1st Ion Energy:	786.4 kJ/mol

Electronegativity:	1.90

Atomic Radius:	117.6 pm

28.0855

-4

+4

Silicon

14

Si

State at 25°C:	solid

Density: 	1.823 g/cm3

Melting Point:	317.3 K

Boiling Point: 	553.7 K

Electron Affinity:	72.07 kJ/mol

1st Ion Energy:	1011.7 kJ/mol

Electronegativity:	2.19

Atomic Radius:	110 pm

30.973762

-3

+3

+5

Phosphorous

15

P

State at 25°C:	solid

Density: 	2.069 g/cm3

Melting Point:	386 K

Boiling Point: 	717.9 K

Electron Affinity:	200.4144 kJ/mol

1st Ion Energy:	999.6 kJ/mol

Electronegativity:	2.58

Atomic Radius:	103 pm

32.066

-2

+2

+4

+6

Sulfur

16

S

State at 25°C:	gas

Density: 	0.0032 g/cm3

Melting Point:	172.22 K

Boiling Point: 	239.2 K

Electron Affinity:	349 kJ/mol

1st Ion Energy:	1251.1 kJ/mol

Electronegativity:	3.16

Atomic Radius:	100 pm

35.4527

-1

+1

+3

+5

+7

Chlorine

17

Cl

State at 25°C:	gas

Density: 	0.0018 g/cm3

Melting Point:	84 K

Boiling Point: 	87.3 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	1520.5 kJ/mol

Electronegativity:

Atomic Radius:	98 pm

39.948

Argon

18

Ar

State at 25°C:	solid

Density: 	0.856 g/cm3

Melting Point:	336.5 K

Boiling Point: 	1038.7 K

Electron Affinity:	48.385 kJ/mol

1st Ion Energy:	418.8 kJ/mol

Electronegativity:	0.82

Atomic Radius:	227 pm

39.098

+1

Potassium

19

K

State at 25°C:	solid

Density: 	1.55 g/cm3

Melting Point:	1112.2 K

Boiling Point: 	1767 K

Electron Affinity:	2.37 kJ/mol

1st Ion Energy:	589.8 kJ/mol

Electronegativity:	1.00

Atomic Radius:	197 pm

40.078

+2

Calcium

20

Ca

State at 25°C:	solid

Density: 	3 g/cm3

Melting Point:	1812.2 K

Boiling Point: 	3021 K

Electron Affinity:	18.1 kJ/mol

1st Ion Energy:	631 kJ/mol

Electronegativity:	1.36

Atomic Radius:	162 pm

44.956

+3

Scandium

21

Sc

State at 25°C:	solid

Density: 	4.5 g/cm3

Melting Point:	1933.2 K

Boiling Point: 	3558 K

Electron Affinity:	7.6 kJ/mol

1st Ion Energy:	658 kJ/mol

Electronegativity:	1.54

Atomic Radius:	147 pm

47.88

+2

+3

+4

Titanium

22

Ti

State at 25°C:	solid

Density: 	6.11 g/cm3

Melting Point:	2163.2 K

Boiling Point: 	3623 K

Electron Affinity:	50.7 kJ/mol

1st Ion Energy:	650.3 kJ/mol

Electronegativity:	1.63

Atomic Radius:	134 pm

50.9415

+2

+3

+5

Vanadium

23

V

State at 25°C:	solid

Density: 	7.14 g/cm3

Melting Point:	2130.2 K

Boiling Point: 	2963 K

Electron Affinity:	64.3 kJ/mol

1st Ion Energy:	652.8 kJ/mol

Electronegativity:	1.66

Atomic Radius:	128 pm

51.9961

+2

+3

+6

Chromium

24

Cr

State at 25°C:	solid

Density: 	7.43 g/cm3

Melting Point:	1517.2 K

Boiling Point: 	2333 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	717.4 kJ/mol

Electronegativity:	1.55

Atomic Radius:	127 pm

54.93

+2

+4

+7

Manganese

25

Mn

State at 25°C:	solid

Density: 	7.874 g/cm3

Melting Point:	1808.2 K

Boiling Point: 	3023 K

Electron Affinity:	15.7 kJ/mol

1st Ion Energy:	759.3 kJ/mol

Electronegativity:	1.90

Atomic Radius:	126 pm

55.85

+2

+3

Iron

26

Fe

State at 25°C:	solid

Density: 	8.9 g/cm3

Melting Point:	1768.2 K

Boiling Point: 	3373 K

Electron Affinity:	63.8 kJ/mol

1st Ion Energy:	758.4 kJ/mol

Electronegativity:	1.88

Atomic Radius:	125 pm

58.93

+2

+3

Cobalt

27

Co

State at 25°C:	solid

Density: 	8.908 g/cm3

Melting Point:	1726.2 K

Boiling Point: 	3193 K

Electron Affinity:	111.5 kJ/mol

1st Ion Energy:	736.7 kJ/mol

Electronegativity:	1.91

Atomic Radius:	124 pm

58.6934

+2

Nickel

28

Ni

State at 25°C:	solid

Density: 	8.95 g/cm3

Melting Point:	1356.6 K

Boiling Point: 	2843 K

Electron Affinity:	118.5 kJ/mol

1st Ion Energy:	745.4 kJ/mol

Electronegativity:	1.95

Atomic Radius:	128 pm

63.546

+1

+2

Copper

29

Cu

State at 25°C:	solid

Density: 	7.14 g/cm3

Melting Point:	692.78 K

Boiling Point: 	1180 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	906.4 kJ/mol

Electronegativity:	1.65

Atomic Radius:	134 pm

65.39

+2

Zinc

30

Zn

State at 25°C:	solid

Density: 	5.904 g/cm3

Melting Point:	302.98 K

Boiling Point: 	2676 K

Electron Affinity:	28.9 kJ/mol

1st Ion Energy:	578.8 kJ/mol

Electronegativity:	1.81

Atomic Radius:	135 pm

69.723

+2

+3

Gallium

31

Ga

State at 25°C:	solid

Density: 	5.323 g/cm3

Melting Point:	1210.6 K

Boiling Point: 	3123 K

Electron Affinity:	119 kJ/mol

1st Ion Energy:	762.1 kJ/mol

Electronegativity:	2.01

Atomic Radius:	122.3 pm

72.61

-4

+2

+4

Germanium

32

Ge

State at 25°C:	solid

Density: 	5.778 g/cm3

Melting Point:	886 K

Boiling Point: 	886.2 K

Electron Affinity:	78 kJ/mol

1st Ion Energy:	946.5 kJ/mol

Electronegativity:	2.18

Atomic Radius:	120 pm

74.92159

-3

+3

+5

Arsenic

33

As

State at 25°C:	solid

Density: 	4.285 g/cm3

Melting Point:	490.2 K

Boiling Point: 	958 K

Electron Affinity:	194.97 kJ/mol

1st Ion Energy:	940.9 kJ/mol

Electronegativity:	2.55

Atomic Radius:	119 pm

78.96

-2

+2

+4

+6

Selenium

34

Se

State at 25°C:	liquid

Density: 	3.1 g/cm3

Melting Point:	266 K

Boiling Point: 	332.7 K

Electron Affinity:	324.7 kJ/mol

1st Ion Energy:	1139.9 kJ/mol

Electronegativity:	2.96

Atomic Radius:	114 pm

79.904

-1

+1

+3

+5

Bromine

35

Br

State at 25°C:	gas

Density: 	0.0037 g/cm3

Melting Point:	116.6 K

Boiling Point: 	119.7 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	1350.7 kJ/mol

Electronegativity:	3.00

Atomic Radius:	112 pm

83.8

+2

Krypton

36

Kr

State at 25°C:	solid

Density: 	1.532 g/cm3

Melting Point:	312.09 K

Boiling Point: 	961 K

Electron Affinity:	46.885 kJ/mol

1st Ion Energy:	403 kJ/mol

Electronegativity:	0.82

Atomic Radius:	248 pm

85.47

+1

Rubidium

37

Rb

State at 25°C:	solid

Density: 	2.63 g/cm3

Melting Point:	1042.2 K

Boiling Point: 	1654 K

Electron Affinity:	5.03 kJ/mol

1st Ion Energy:	549.5 kJ/mol

Electronegativity:	0.95

Atomic Radius:	215 pm

87.62

+2

Strontium

38

Sr

State at 25°C:	solid

Density: 	4.5 g/cm3

Melting Point:	1796.2 K

Boiling Point: 	3537 K

Electron Affinity:	29.6 kJ/mol

1st Ion Energy:	615.6 kJ/mol

Electronegativity:	1.22

Atomic Radius:	180 pm

88.90585

+3

Yittrium

39

Y

State at 25°C:	solid

Density: 	6.51 g/cm3

Melting Point:	2125.2 K

Boiling Point: 	4473 K

Electron Affinity:	41.1 kJ/mol

1st Ion Energy:	660 kJ/mol

Electronegativity:	1.33

Atomic Radius:	160 pm

91.224

+4

Zirconium

40

Zr

State at 25°C:	solid

Density: 	8.57 g/cm3

Melting Point:	2741.2 K

Boiling Point: 	5031 K

Electron Affinity:	86.2 kJ/mol

1st Ion Energy:	663.8 kJ/mol

Electronegativity:	1.60

Atomic Radius:	146 pm

92.90638

+5

Niobium

41

Nb

State at 25°C:	solid

Density: 	10.28 g/cm3

Melting Point:	2890.2 K

Boiling Point: 	4923 K

Electron Affinity:	72 kJ/mol

1st Ion Energy:	684.9 kJ/mol

Electronegativity:	2.24

Atomic Radius:	139 pm

95.94

+4

+6

Molybdenum

42

Mo

State at 25°C:	solid

Density: 	11.5 g/cm3

Melting Point:	2445.2 K

Boiling Point: 	4840 K

Electron Affinity:	53 kJ/mol

1st Ion Energy:	702.4 kJ/mol

Electronegativity:	1.90

Atomic Radius:	136 pm

[97.907]

+4

+7

Technetium

43

Tc

State at 25°C:	solid

Density: 	12.41 g/cm3

Melting Point:	2583.2 K

Boiling Point: 	4323 K

Electron Affinity:	101 kJ/mol

1st Ion Energy:	711.1 kJ/mol

Electronegativity:	2.20

Atomic Radius:	134 pm

101.07

+3

+4

Ruthenium

44

Ru

State at 25°C:	solid

Density: 	12.39 g/cm3

Melting Point:	2238.2 K

Boiling Point: 	4033 K

Electron Affinity:	109.7 kJ/mol

1st Ion Energy:	719.8 kJ/mol

Electronegativity:	2.28

Atomic Radius:	134 pm

102.9055

+3

Rhodium

45

Rh

State at 25°C:	solid

Density: 	11.99 g/cm3

Melting Point:	1827.2 K

Boiling Point: 	3213 K

Electron Affinity:	53.7 kJ/mol

1st Ion Energy:	804.7 kJ/mol

Electronegativity:	2.20

Atomic Radius:	137 pm

106.42

+2

+4

Palladium

46

Pd

State at 25°C:	solid

Density: 	10.49 g/cm3

Melting Point:	1235.1 K

Boiling Point: 	2428 K

Electron Affinity:	125.6 kJ/mol

1st Ion Energy:	731 kJ/mol

Electronegativity:	1.93

Atomic Radius:	144 pm

107.8682

+1

Silver

47

Ag

State at 25°C:	solid

Density: 	8.65 g/cm3

Melting Point:	594.1 K

Boiling Point: 	1038 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	867.7 kJ/mol

Electronegativity:	1.69

Atomic Radius:	151 pm

112.411

+2

Cadmium

48

Cd

State at 25°C:	solid

Density: 	7.31 g/cm3

Melting Point:	429.81 K

Boiling Point: 	2353 K

Electron Affinity:	28.9 kJ/mol

1st Ion Energy:	558.3 kJ/mol

Electronegativity:	1.78

Atomic Radius:	167 pm

114.82

+3

Indium

49

In

State at 25°C:	solid

Density: 	7.265 g/cm3

Melting Point:	505.168 K

Boiling Point: 	2896 K

Electron Affinity:	107.3 kJ/mol

1st Ion Energy:	708.6 kJ/mol

Electronegativity:	1.88

Atomic Radius:	140.5 pm

118.71

-4

+2

+4

Tin

50

Sn

State at 25°C:	solid

Density: 	6.697 g/cm3

Melting Point:	903.94 K

Boiling Point: 	1860 K

Electron Affinity:	103 kJ/mol

1st Ion Energy:	833.7 kJ/mol

Electronegativity:	2.05

Atomic Radius:	140 pm

121.57

-3

+3

+5

Antimony

51

Sb

State at 25°C:	solid

Density: 	6.25 g/cm3

Melting Point:	722.7 K

Boiling Point: 	1263 K

Electron Affinity:	190.16 kJ/mol

1st Ion Energy:	869.2 kJ/mol

Electronegativity:	2.10

Atomic Radius:	142 pm

127.6

-2

+2

+4

+6

Tellurium

52

Te

State at 25°C:	solid

Density: 	4.94 g/cm3

Melting Point:	386.7 K

Boiling Point: 	458.4 K

Electron Affinity:	295.16 kJ/mol

1st Ion Energy:	1008.4 kJ/mol

Electronegativity:	2.66

Atomic Radius:	133 pm

126.90447

-1

+1

+3

+5

+7

Iodine

53

I

State at 25°C:	gas

Density: 	0.0059 g/cm3

Melting Point:	161.3 K

Boiling Point: 	165 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	1170.4 kJ/mol

Electronegativity:	2.60

Atomic Radius:	131 pm

131.29

+2

+4

+6

Xenon

54

Xe

State at 25°C:	solid

Density: 	1.9 g/cm3

Melting Point:	301.6 K

Boiling Point: 	978 K

Electron Affinity:	45.506 kJ/mol

1st Ion Energy:	375.7 kJ/mol

Electronegativity:	0.79

Atomic Radius:	265 pm

132.90543

+1

Cesium

55

Cs

State at 25°C:	solid

Density: 	3.62 g/cm3

Melting Point:	998.2 K

Boiling Point: 	2123 K

Electron Affinity:	13.95 kJ/mol

1st Ion Energy:	502.9 kJ/mol

Electronegativity:	0.89

Atomic Radius:	222 pm

137.327

+2

Barium

56

Ba

State at 25°C:	solid

Density: 	6.17 g/cm3

Melting Point:	1193.2 K

Boiling Point: 	3693 K

Electron Affinity:	48 kJ/mol

1st Ion Energy:	538.1 kJ/mol

Electronegativity:	1.10

Atomic Radius:	187 pm

138.91

+3

Lanthanium

57

La

State at 25°C:	solid

Density: 	6.773 g/cm3

Melting Point:	1071.2 K

Boiling Point: 	3743 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	527.4 kJ/mol

Electronegativity:	1.12

Atomic Radius:	182 pm

140.115

+3

+4

Cerium

58

Ce

State at 25°C:	solid

Density: 	6.475 g/cm3

Melting Point:	1204.2 K

Boiling Point: 	3293 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	523.2 kJ/mol

Electronegativity:	1.13

Atomic Radius:	182 pm

140.90765

+3

Praseodymium

59

Pr

State at 25°C:	solid

Density: 	7.003 g/cm3

Melting Point:	1283.2 K

Boiling Point: 	3300 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	529.6 kJ/mol

Electronegativity:	1.14

Atomic Radius:	181 pm

144.24

+3

Neodymium

60

Nd

State at 25°C:	solid

Density: 	7.2 g/cm3

Melting Point:	1353.2 K

Boiling Point:

Electron Affinity:	50 kJ/mol

1st Ion Energy:	535.9 kJ/mol

Electronegativity:	1.15

Atomic Radius:	183 pm

144.9128

+3

Promethium

61

Pm

State at 25°C:	solid

Density: 	7.536 g/cm3

Melting Point:	1345.2 K

Boiling Point: 	2073 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	543.3 kJ/mol

Electronegativity:	1.17

Atomic Radius:	180 pm

150.36

+3

Samarium

62

Sm

State at 25°C:	solid

Density: 	5.245 g/cm3

Melting Point:	1095.2 K

Boiling Point: 	1712 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	546.7 kJ/mol

Electronegativity:	1.12

Atomic Radius:	208 pm

151.965

+2

+3

Europium

63

Eu

State at 25°C:	solid

Density: 	7.886 g/cm3

Melting Point:	1584.2 K

Boiling Point: 	3273 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	592.6 kJ/mol

Electronegativity:	1.17

Atomic Radius:	180 pm

157.25

+3

Gadolinium

64

Gd

State at 25°C:	solid

Density: 	8.253 g/cm3

Melting Point:	1633.2 K

Boiling Point: 	3073 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	564.7 kJ/mol

Electronegativity:	1.21

Atomic Radius:	177 pm

158.92534

+3

Terbium

65

Tb

State at 25°C:	solid

Density: 	8.559 g/cm3

Melting Point:	1682.2 K

Boiling Point: 	2873 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	571.9 kJ/mol

Electronegativity:	1.20

Atomic Radius:	178 pm

162.5

+3

Dysprosium

66

Dy

State at 25°C:	solid

Density: 	8.78 g/cm3

Melting Point:	1743.2 K

Boiling Point: 	2873 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	580.7 kJ/mol

Electronegativity:	1.23

Atomic Radius:	176 pm

164.9032

+3

Holmium

67

Ho

State at 25°C:	solid

Density: 	9.045 g/cm3

Melting Point:	1795.2 K

Boiling Point: 	3173 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	588.7 kJ/mol

Electronegativity:	1.24

Atomic Radius:	176 pm

167.26

+3

Erbium

68

Er

State at 25°C:	solid

Density: 	9.318 g/cm3

Melting Point:	1818.2 K

Boiling Point: 	2000 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	596.7 kJ/mol

Electronegativity:	1.25

Atomic Radius:	176 pm

168.934

+3

Thulium

69

Tm

State at 25°C:	solid

Density: 	6.973 g/cm3

Melting Point:	1097.2 K

Boiling Point: 	1700 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	603.4 kJ/mol

Electronegativity:	1.21

Atomic Radius:	193 pm

173.04

+3

Ytterbium

70

Yb

State at 25°C:	solid

Density: 	9.84 g/cm3

Melting Point:	1929.2 K

Boiling Point: 	3600 K

Electron Affinity:	50 kJ/mol

1st Ion Energy:	523.6 kJ/mol

Electronegativity:	1.27

Atomic Radius:	174 pm

174.967

+3

Lutetium

71

Lu

State at 25°C:	solid

Density: 	13.28 g/cm3

Melting Point:	2495.2 K

Boiling Point: 	4723 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	680 kJ/mol

Electronegativity:	1.30

Atomic Radius:	159 pm

178.49

+4

Hafnium

72

Hf

State at 25°C:	solid

Density: 	16.65 g/cm3

Melting Point:	3269.2 K

Boiling Point: 	5807 K

Electron Affinity:	31.1 kJ/mol

1st Ion Energy:	761 kJ/mol

Electronegativity:	1.50

Atomic Radius:	146 pm

180.9479

+5

Tantalum

73

Ta

State at 25°C:	solid

Density: 	19.3 g/cm3

Melting Point:	3683.2 K

Boiling Point: 	5773 K

Electron Affinity:	78.6 kJ/mol

1st Ion Energy:	770 kJ/mol

Electronegativity:	2.36

Atomic Radius:	139 pm

183.85

+4

+6

Tungsten

74

W

State at 25°C:	solid

Density: 	21 g/cm3

Melting Point:	3453.2 K

Boiling Point: 	5923 K

Electron Affinity:	14.5 kJ/mol

1st Ion Energy:	760 kJ/mol

Electronegativity:	1.90

Atomic Radius:	137 pm

186.2

+4

Rhenium

75

Re

State at 25°C:	solid

Density: 	22.57 g/cm3

Melting Point:	3318.2 K

Boiling Point: 	5298 K

Electron Affinity:	106.1 kJ/mol

1st Ion Energy:	840 kJ/mol

Electronegativity:	2.20

Atomic Radius:	135 pm

190.2

+4

Osmium

76

Os

State at 25°C:	solid

Density: 	22.61 g/cm3

Melting Point:	2683.2 K

Boiling Point: 	4823 K

Electron Affinity:	151 kJ/mol

1st Ion Energy:	880 kJ/mol

Electronegativity:	2.20

Atomic Radius:	136 pm

192.22

+3

+4

Iridium

77

Ir

State at 25°C:	solid

Density: 	21.41 g/cm3

Melting Point:	2045.2 K

Boiling Point: 	4443 K

Electron Affinity:	205.3 kJ/mol

1st Ion Energy:	870 kJ/mol

Electronegativity:	2.28

Atomic Radius:	139 pm

195.08

+2

+4

Platinum

78

Pt

State at 25°C:	solid

Density: 	19.32 g/cm3

Melting Point:	1337.63 K

Boiling Point: 	3081 K

Electron Affinity:	222.752 kJ/mol

1st Ion Energy:	890.1 kJ/mol

Electronegativity:	2.54

Atomic Radius:	144 pm

196.96654

+1

+3

Gold

79

Au

State at 25°C:	liquid

Density: 	13.534 g/cm3

Melting Point:	234.33 K

Boiling Point: 	630 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	1007 kJ/mol

Electronegativity:	2.00

Atomic Radius:	151 pm

200.59

+1

+2

Mercury

80

Hg

State at 25°C:	solid

Density: 	11.85 g/cm3

Melting Point:	576.7 K

Boiling Point: 	1730 K

Electron Affinity:	19.2 kJ/mol

1st Ion Energy:	589.4 kJ/mol

Electronegativity:	1.83

Atomic Radius:	170 pm

204.383

+1

+3

Thallium

81

Tl

State at 25°C:	solid

Density: 	11.342 g/cm3

Melting Point:	600.702 K

Boiling Point: 	2024 K

Electron Affinity:	35.1 kJ/mol

1st Ion Energy:	715.6 kJ/mol

Electronegativity:	2.10

Atomic Radius:	146 pm

207.2

+2

+4

Lead

82

Pb

State at 25°C:	solid

Density: 	9.808 g/cm3

Melting Point:	544.5 K

Boiling Point: 	1837 K

Electron Affinity:	91.3 kJ/mol

1st Ion Energy:	703.3 kJ/mol

Electronegativity:	2.02

Atomic Radius:	150 pm

208.98037

+3

Bismuth

83

Bi

State at 25°C:	solid

Density: 	9.142 g/cm3

Melting Point:	527.2 K

Boiling Point: 	1235 K

Electron Affinity:	183.3 kJ/mol

1st Ion Energy:	812 kJ/mol

Electronegativity:	2.00

Atomic Radius:	168 pm

[208.98]

-2

+2

+4

Polonium

84

Po

State at 25°C:	solid

Density: 	~7 g/cm3

Melting Point:	575.2 K

Boiling Point: 	610.15 K

Electron Affinity:	270.1 kJ/mol

1st Ion Energy:	890 kJ/mol

Electronegativity:	2.20

Atomic Radius:

[209.98]

-1

+1

Astatine

85

At

State at 25°C:	gas

Density: 	0.0097 g/cm3

Melting Point:	202.2 K

Boiling Point: 	211 K

Electron Affinity:	0 kJ/mol

1st Ion Energy:	1037 kJ/mol

Electronegativity:

Atomic Radius:	120 pm

[222.02]

Radon

86

Rn

State at 25°C:	solid

Density: 	1.87 g/cm3

Melting Point:	300.2 K

Boiling Point: 	950.15 K

Electron Affinity:

1st Ion Energy:	384 kJ/mol

Electronegativity:	0.7

Atomic Radius:

[223.02]

+1

Francium

87

Fr

State at 25°C:	solid

Density: 	5.5 g/cm3

Melting Point:	973.2 K

Boiling Point: 	1973 K

Electron Affinity:

1st Ion Energy:	509.4 kJ/mol

Electronegativity:	0.9

Atomic Radius:	215 pm

[226.03]

+2

Radium

88

Ra

State at 25°C:	solid

Density: 	10.07 g/cm3

Melting Point:	1323.2 K

Boiling Point: 	2743 K

Electron Affinity:

1st Ion Energy:	499 kJ/mol

Electronegativity:	1.1

Atomic Radius:	195 pm

[227.03]

+3

Actinium

89

Ac

State at 25°C:	solid

Density: 	11.78 g/cm3

Melting Point:	2023.2 K

Boiling Point: 	5123 K

Electron Affinity:

1st Ion Energy:	587 kJ/mol

Electronegativity:	1.3

Atomic Radius:	179 pm

232.0381

+4

Thorium

90

Th

State at 25°C:	solid

Density: 	15.37 g/cm3

Melting Point:	1873.2 K

Boiling Point: 	4500 K

Electron Affinity:

1st Ion Energy:	568 kJ/mol

Electronegativity:	1.5

Atomic Radius:	163 pm

231.03588

+5

Protactinium

91

Pa

State at 25°C:	solid

Density: 	19.05 g/cm3

Melting Point:	1405.2 K

Boiling Point: 	4203 K

Electron Affinity:

1st Ion Energy:	584 kJ/mol

Electronegativity:	1.7

Atomic Radius:	156 pm

238.03

+6

Uranium

92

U

State at 25°C:	solid

Density: 	20.45 g/cm3

Melting Point:	913.2 K

Boiling Point: 	4175 K

Electron Affinity:

1st Ion Energy:	597 kJ/mol

Electronegativity:	1.3

Atomic Radius:	155 pm

[237.05]

+5

Neptunium

93

Np

State at 25°C:	solid

Density: 	19.86 g/cm3

Melting Point:	914.2 K

Boiling Point: 	3503 K

Electron Affinity:

1st Ion Energy:	585 kJ/mol

Electronegativity:	1.3

Atomic Radius:	159 pm

[244.06]

+4

Plutonium

94

Pu

State at 25°C:	solid

Density: 	13.67 g/cm3

Melting Point:	1267.2 K

Boiling Point: 	2873 K

Electron Affinity:

1st Ion Energy:	578 kJ/mol

Electronegativity:	1.3

Atomic Radius:	173 pm

[243.06]

+3

Americium

95

Am

State at 25°C:	solid

Density: 	13.51 g/cm3

Melting Point:	1613.2 K

Boiling Point:

Electron Affinity:

1st Ion Energy:	581 kJ/mol

Electronegativity:	1.3

Atomic Radius:	174 pm

[247.07]

+3

Curium

96

Cm

State at 25°C:	solid

Density: 	14.78 g/cm3

Melting Point:	1259.2 K

Boiling Point:

Electron Affinity:

1st Ion Energy:	601 kJ/mol

Electronegativity:	1.3

Atomic Radius:	170 pm

[247.07]

+3

Berkelium

97

Bk

State at 25°C:

Density: 	15.1 g/cm3

Melting Point:	1173.2 K

Boiling Point:

Electron Affinity:

1st Ion Energy:	608 kJ/mol

Electronegativity:	1.3

Atomic Radius:	186 pm

[251.08]

+3

Californium

98

Cf

State at 25°C:

Density: 	~13.5 g/cm3

Melting Point:	1133.2 K

Boiling Point:

Electron Affinity:

1st Ion Energy:	619 kJ/mol

Electronegativity:	1.3

Atomic Radius:	186 pm

[252.08]

+3

Einsteinium

99

Es

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:	627 kJ/mol

Electronegativity:	1.3

Atomic Radius:

[257.10]

+3

Fermium

100

Fm

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:	635 kJ/mol

Electronegativity:	1.3

Atomic Radius:

[258.10]

+3

Mendelevium

101

Md

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:	642 kJ/mol

Electronegativity:	1.3

Atomic Radius:

[259.10]

+2

Nobelium

102

No

State at 25°C:

Density: 	>9.84 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[262.11]

+3

Lawrencium

103

Lr

State at 25°C:

Density: 	18.1 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[265.12]

+4

Rutherfordium

104

Rf

State at 25°C:

Density: 	~39 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[268.13]

+5

Dubnium

105

Db

State at 25°C:

Density: 	~35 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[271.12]

+6

Seaborgium

106

Sg

State at 25°C:

Density: 	~37 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[270]

+7

Bohrium

107

Bh

State at 25°C:

Density: 	~41 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[277.15]

+8

Hassium

108

Hs

State at 25°C:

Density: 	~35 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[276.15]

Meitnerium

109

Mt

State at 25°C:

Density: 	>21.46 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[281.16]

Darmstadtium

110

Ds

State at 25°C:

Density: 	>19.282 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[280.16]

Roentgenium

111

Rg

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[285.17]

Copernicum

112

Cn

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[284.18]

Ununtrium

113

Uut

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[289.19]

Flerovium

114

Fl

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[288.19]

Ununpentium

115

Uup

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[293]

Livermorium

116

Lv

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[294]

Ununseptium

117

Uus

State at 25°C:

Density: 	 g/cm3

Melting Point:

Boiling Point:

Electron Affinity:

1st Ion Energy:

Electronegativity:

Atomic Radius:

[294]

Ununoctium

118

Uuo